SECTION 10 51 13

METAL LOCKERS

PART 1 – GENERAL

1.01 	SECTION INCLUDES

A. 	Standard Duty Knocked Down Lockers

B. 	Locker benches.

1.02	REFERENCES

A.	ADAAG - Americans with Disabilities Act, Accessibility Guidelines.

1.03	SUBMITTALS

A.	Submit under provisions of Section 01 33 00.

B.	Manufacturer's data sheets on each product to be used, including:

1.	Preparation instructions and recommendations.

2.	Storage and handling requirements and recommendations.

3.	Installation methods.

C.	Shop Drawings: Show the following:

1.	Dimensioned drawings including plans, elevations, and sections to show locker locations and interfaces with adjacent substrates.

2.	Details of assembly, erection, anchorage and clearance requirements.

D. 	Selection Samples: For each finish product specified, supply paint on paper chips in

the chosen color(s), representing manufacturer's color and finish.

1.04	DELIVERY, STORAGE, AND HANDLING

A.	Store products in manufacturer's unopened packaging until ready for installation.

B.	Protect locker finish and adjacent surfaces from damage.

PART 2 - PRODUCTS

2.01	MANUFACTURERS

A.	Acceptable Manufacturer: Penco Products, Inc., which is located at: 1820 Stonehenge Drive, Greenville, NC 27858; Tel: 800-562-1000; Fax: 800-248-1555; Email: general@pencoproducts.com; Web: www.pencoproducts.com

B.	Lockers shall be GREENGUARD Gold Certified by UL Environment through the GREENGUARD Certification Program.

  - MATERIALS

- Steel: Prime grade mild cold-rolled sheet steel free from surface imperfection, capable of taking a high-grade enamel finish and in compliance with ASTM A1008.

- Steel: Sheet steel components shall be fabricated using zinc-coated steel free from surface imperfection, capable of taking a high-grade enamel finish and in compliance with ASTM A653.

- Bolts and Nuts: Zinc plated truss fin head bolts and hex nuts.

- Provide only metal lockers fabricated in the United States by a single domestic 		manufacturer.

2.03	STANDARD DUTY LOCKERS

A.	Standard Duty Lockers:

1.	Acceptable Product:  Penco Vanguard, knock-down lockers.

2.	Tops, Bottoms, Backs, Sides, and Shelves:  24-gauge sheet steel.

3.	Doors 20-inches or higher are 16-gauge sheet steel.

4.	Doors smaller than 20-inches high (box doors) are 18-gauge sheet steel.

5.	Legs: 6 inches (150 mm) high (standard).

6.	No legs (optional).

B. 	Locker Body: Steel specially formed for added strength and rigidity and to ensure 						tight joints at fastening points.

1.	Tops and bottoms with four sides formed 90 degrees, the front offset formed 							to be flush with horizontal frame member.

2.	Shelves with four sides formed to 90 degrees, front edge having a second 							bend.

3.	Hole spacing in locker body construction:  Not exceeding 9 inches (225 mm).

4.	Form door frame members to a channel shape, not less than 16-gauge steel.

5.	Provide vertical door frame members with additional 3/8 inch (9.5 mm) flange 							as a continuous door strike.

6.	Securely weld cross frame members of channel shapes to vertical framing 							members to ensure rigidity, including intermediate cross frame on double and 							triple tier lockers.

7.	Optional factory assembly of locker bodies using rivets.

8.	Center partitions:  24-gauge steel vertical partitions, full depth between 								bottom and shelf.

C.	Locker Doors: One-piece sheet steel.

1.	Multi-Point Latch Doors:  Full channel formation of adequate depth to fully 							conceal lock bar on lock side, channel formation on hinge side, right angle 							formations across top and bottom, with holes for attaching number plates.

2.	Provide holes for attaching number plates.

3.	Doors 18 inches (457.2 mm) or wider by 36 inches (914.4 mm) high or higher:

3 inch (76 mm) wide 20-gauge full height reinforcing pan 						welded to inside face of door at 6 inch (152 mm) centers.

4.	Box Lockers: Channel formations on lock and hinge sides, right angle flanges 							on top and bottom; pre-punch doors for padlock latch and friction catch and 							built-in combination and key locks.

5.	Ventilation:  Provide louvered doors in manufacturer's standard louver 								pattern.

a.	Doors 60 inches (1524 mm) or Higher:  Louvers in groups of 6 at top 								and bottom.

b.	36 inch (914 mm) High Doors:  3 and 6 louvers.

c.	30 inch (762 mm) High Doors:  Minimum one group of 6 louvers.

d.	24 inch (610 mm) High Doors:  Minimum one group of 3 louvers.

D.	Hinges:

1.	Two-inch high, 0.074 inch (1.88 mm) thick sheet steel, double spun, full loop, 							tight pin, projection welded to door frame and securely fastened to the door 							with two aluminum rivets.

a.	Doors 48 inches (1219 mm) or higher: Three 2 inch (51 mm) high five-							knuckle hinges.

b.        84 inch (2134 mm) high doors: Four 2 inch (51 mm) high five-knuckle hinges.

c.	All other doors: Two 2 inch (51 mm) high five-knuckle hinges.

d.	Optional: 16ga continuous hinge, full height of door.

2.04	DOOR HANDLES AND LATCHING

A.	Two Person and Duplex Lockers, 1, 2 and 3 Tier:  Multi-point latching:

1.	Chrome-plated zinc alloy die-cast case and handle, 40,000 psi (276 MPa) 							maximum tensile strength.

2.	Attachment to latch bar concealed inside door and tamperproof; pulling 								handle out shall move latch bar up and open door in one motion.

3.	Padlock Eye:  For use with 9/32 inch (7.1 mm) diameter padlock, integral with 							handle and located so that extension of handle forms padlock strike.

4.	Case:  Kick-proof type shielding movable part and providing padlock strike to 							prevent scratching and marring the door.

5.	Provide lock hole cover plate for use with padlocks.

6.	Latch Clip:  Glass-filled nylon engaging the door frame and holding the door 							shut.

a.	Doors 48 inches (1219 mm) and higher:  Three points.

b.	All other Doors:  Two points.

7.	Locking Device:  Positive, automatic type, whereby locker may be locked 							when open, then closed without unlocking.

8.	Firmly secure rubber silencers in frame as required by manufacturer.

9.	Classic III Multi-point latching with recessed handles:

a.	Recess finger-lift control handle in door.

b.	Pocket:  brushed stainless steel securely fastened to door with two tabs and 							a positive tamper-resistant decorative fastener; of depth sufficient to prevent a 							combination padlock, built-in combination lock, or key lock from protruding beyond door 					face.

c.	Provide lock hole cover plate for use with padlocks.

d.	Attach formed steel lifting piece to latching channel with one 							       		concealed retaining lug and one rivet, assuring a positive two-point 								connection.

e.	Handle finger lift: Molded, sound-deadening, attached with rivet; 									padlock eye for use with 9/32 inch (7.1 mm) diameter padlock shackle.

f.	Latch Clip:  Glass-filled nylon engaging the door frame and holding the 								door shut.

1)	Doors 48 inches (1219 mm), 60 inches and 72 inches (1829 mm) high: Three 							points.

2)	Doors 42-inch, 36-inch, 30-inch, 24-inch and 20-inch: Two points.

g.	Locking Device: Positive, automatic type, whereby locker may be 								locked when open, then closed without unlocking.

h.	Firmly secure rubber silencers in frame as required by manufacturer.

B.	Box Lockers (3 to 9 Tier):

1.	Punch doors for use with padlocks or built-in locks.

2.	Equip doors for use with padlocks with an 18-gauge combination door pull, 							staple, and lock hole cover plate with integral friction catch.

2.05	INTERIOR EQUIPMENT

- Single Tier lockers 48.5 inch or higher shall have a hat shelf located approximately 9-inches below

the top of the locker. If less than 18-inch deep, locker shall have three single prong hooks and one double prong ceiling prong hooks on 9-inch and 12-inch wide lockers. Four single prong hooks are supplied in wider models. Single tier lockers 18 inches or more in depth shall have a coat rod instead of a ceiling hook. 30 inches and 36 inches high lockers shall have three single prong wall hooks and one double prong ceiling hook through 12-inch wide and four wall hooks for 15 inch or wider. 24-inch wide will have two double prong ceiling hooks. 20-inch and 24-inch high openings to have three wall hooks through 12-inch wide and four wall hooks for 15-inch wide or wider. Hooks to be attached with two bolts per hooks.

B.	ADA-Compliant Lockers (Recessed Handles with Multi-Point Latch):

1.	Single Tier Lockers:  Hat shelf 48 inches (1.219 m) maximum off the floor.

2.	Locker Compartment Bottom:  Minimum of 15 inches (230 mm) off the floor, 
or an extra shelf placed 15 inches (381 mm) off the floor for unobstructed 
forward and side reach.

3.	Handicapped symbol attached to door.

4.	Hooks and rods as specified for other lockers.

2.06	ACCESSORIES

A.	Number Plates: Provide each locker with a polished aluminum number plate, 2-1/4 						inches (57 mm) wide by 1 inch (25 mm) high, with black numerals not less than 3/8 						inch (9.5 mm) high; attach to face of door with two aluminum rivets.

B.	Closed Bases: 18-gauge closed metal front and end bases, finished to match 							lockers.

C.	Locks: Built-in flat key locks; master-key to same series.

D. 	Locks: Built-in grooved key locks (pin tumbler); master-key to same series.

E.	Locks: Built-in three-number dialing combination locks capable of at least five 							different combinations changes; provide master key, combination change key, and 						combination control charts.

F. 	Padlocks: Master-keyed three-number dialing combination type padlocks; provide 						master key. Mechanism must be resistant to “shimming”.

G.	Continuous Sloped Hoods: 18-gauge steel, slope rise equal to 1/3 of the locker 						depth (18.5 degrees), plus a 1 inch (25 mm) vertical rise at front.

1.	Supplied in 72 inch (1829 mm) lengths only.

2.	Slip joints without visible fasteners at splice locations.

3.	Provide necessary end closures.

4.	Finish to match lockers.

H.        Continuous Sloped Hoods: 16-gauge steel, slope rise equal to 1/3 of the locker 						depth (18.5 degrees), plus a 1 inch (25 mm) vertical rise at front.

1.	Supplied in 72 inch (1829 mm) lengths only.

2.	Slip joints without visible fasteners at splice locations.

3.	Provide necessary end closures.

4.	Finish to match lockers.

I.	Unit Slope Tops for Standard Duty Lockers: 24-gauge steel, slope rise equal to 1/3 						of the locker depth, finish to match lockers.

J.	Box Finished End Panels: Minimum 16-gauge steel formed to match locker depth and 					height, 1 inch (25 mm) edge dimension; finish to match lockers; install with 							concealed fasteners.

K.	Vertical Fillers: 20-gauge steel formed in an angle shape, with 20-gauge slip joint angles formed in an angle shape with double bend on one leg forming a pocket to provide adjustable mating with angle filler.

1.	Attachment by means of concealed fasteners.

2.	Finish to match lockers.

3.	Optional 16-gauge available.

L.	Zee Bases for Knock-Down Lockers: 14 gauge, steel flanged outward at top for 						support of lockers, flanged inward at bottom for anchoring to floor.

1.	Height:  4 inches (101 mm).

2.	Height:  6 inches (150 mm).

M.	Recess Trim: 18-gauge steel, 3 inch (75 mm) face dimension.

1.	Vertical and/or horizontal as required.

2.	Standard lengths as long as practical.

3.	Attach to lockers with concealed clips.

4.	Provide necessary finish caps and splices.

5.	Finish to match lockers.

N.	Benches: Laminated selected hardwood, 1-1/4 inch (31 mm) full finished thickness, 						corners rounded and sanded, surfaces finished with two coats of clear lacquer.

1.	Depth: 9-1/2 inches (240 mm) deep.

2.	Depth: 12 inches (305 mm) deep.

3.	Depth: 24 inches (610 mm) deep.

4.	Lengths:  As shown.

O.	Heavy-Duty Bench Pedestals: Steel tubing with 11-gauge steel flanges welded to 						each end, 16-1/4 inches (412 mm) high, finish to match lockers.

P.	Stainless Steel Free-Standing Bench Pedestals: 2-inch (50 mm) diameter brushed 						16-gauge stainless steel formed into a trapezoid, 14 inch (355 mm) wide bottom with 						two 5/16 inch (7.9 mm) diameter holes, top flange with four 5/16 inch (7.9 mm) 						diameter holes for fastening to bench. (Not recommended for use on ADA complaint benches)

2.07	FABRICATION

A.	Fabricate lockers square and rigid, without warp, with metal faces flat and free of distortion.

B.	Knock-Down Lockers: Fabricate lockers on the unit principle, each locker with 							individual door and frame, individual top, bottom, back, and shelves, with common 						intermediate divisions separating compartments.  Verify dimensions and arrangement before 				fabrication.

C.	Finish: Hybrid Polyester powder coat paint finish electrostatically applied and properly cured to 					manufacturer’s specifications for optimum performance. Finishes containing volatile organic 				compounds and subject to out-gassing are not acceptable.

      - Powder Coat - Dry Thickness: 1 to 1.2 mils (0.025 to 0.03 mm).

      - Powder Coat Plus - Dry Thickness: 2 to 2.2 mils (0.05 to 0.055 mm).

      - Color:  As selected from manufacturer's standard colors.

      - Special Finish

        - Custom color

        - Anti-Graffiti

        - Anti-Microbial

      - Most Vanguard locker sizes are based on using Common Color Body Parts, 073 Champagne for

body and the door and frame is painted in the Penco color selected.

PART 3 – EXECUTION

3.01	EXAMINATION

A.	Do not begin installation until substrates and bases have been properly prepared.

B.	If substrate and bases are the responsibility of another installer, notify Architect of 						unsatisfactory preparation before proceeding.

3.02	INSTALLATION

A.	Install metal lockers and accessories at locations shown in accordance with 							manufacturer's instructions.

B.	Install lockers plumb, level, and square.

C.	Anchor lockers to floor and wall at 48 inches (1.219 m) or less, as recommended by 						the manufacturer.

D.	Backing / Blocking locations are provided at the sole discretion of the installer for a secure and proper installation. Backing/Blocking locations are provided at the sole discretion of the installer for a secure installation.

E.	Bolt adjoining locker units together to provide rigid installation.

F.	Install sloping tops and metal fillers using concealed fasteners.  Provide flush 							hairline joints against adjacent surfaces.

G.	Install front bases between legs without overlap or exposed fasteners.  Provide end 						bases on exposed ends.

H.	Install benches by fastening bench tops to pedestals and securely anchoring to the 						floor using appropriate anchors for the floor material.

3.03	ADJUSTING AND CLEANING

A.	Adjust doors and latches to operate without binding.  Verify that latches are 							operating satisfactorily.

B.       Adjust built-in locks to prevent binding of dial or key and ensure smooth operation 						prior to substantial completion.

C.	Touch-up with factory-supplied paint and repair or replace damaged products before 						Substantial Completion.

3.04	PROTECTION

A.	Protect installed products until completion of project.

END OF SECTION